SECTION 07500

GMX HOT-APPLIED WATERPROOFING SPECIFICATION

PART 1 – GENERAL

1.0		DESCRIPTION

These specifications are presented as a guide for the application of the GMX Hot Applied Waterproofing System. All materials used in this application must be supplied or approved by GMX.  Any questions should be directed to GMX.

2.0 	QUALITY ASSURANCE

- All products shall be produced or approved by GMX.

- The system shall be installed by an approved GMX applicator.

- All materials shall be installed as per accepted roofing practice and in strict accordance with GMX’s written specifications.  Any deviation must be approved in writing by GMX.

3.0	DELIVERY, STORAGE AND HANDLING

A.	All materials, except bulk deliveries, shall be delivered in the manufacturer's original container.  The containers shall be sealed and display the manufacturer's original label(s).

- All liquid materials shall be stored in a cool, dry, shaded area during hot weather or in a dry, heated area during cold weather.  Roll goods and granules shall be stored in a clean, temperature controlled area.  Any materials exposed to the elements shall be elevated above the ground and covered by a tarpaulin.  Materials must not be exposed to excessive heat or direct flame.

C.	Materials shall be handled so as to minimize damage or contamination with moisture or foreign matter.  Solvent-based materials are combustible.  Keep containers closed when the materials are not in use.  Wear sunglasses to prevent eye damage and use suntan lotion to prevent sunburn when applying reflective coatings.

4.0	JOB CONDITIONS

A.	Wateproofing materials shall not be applied during inclement weather and the installation shall not proceed in the event that precipitation is probable during application.

B.	Coatings shall be stored at room temperature until immediately prior to use when the ambient temperature is 40 F. or below, including wind chill.  Discontinue the application of coatings if the material can not be stored at temperatures which permit even distribution during application.

C.	When applying materials with spray equipment, take precautions to prevent overspray from damaging or defacing surrounding walls, building surfaces, vehicles or other property.

D.	Avoid inhaling spray mist; take precautions to ensure adequate ventilation.

E.	The completed roof system must be protected from foot traffic until fully cured.

5.0	MATERIALS

A.	All materials used in GMX Hot-Applied Waterproofing System shall be produced or approved by GMX, including:

1.   	GMX SEBS Modified Asphalt

2.  	GMX Hot-Applied Polyester (optional)

3.  	Ultra-Shield Non-Fibered Aluminum

4.   	Ultra-Shield Fibered Aluminum Coating

5.   	Ultra-Shield Roof Primer

6.   	Ultra-Shield Plastic Roof Cement

7.  	Ultra-Shield Rubberized Cement

8.   	Ultra-Shield Built-Up Mastic

9.   	Ultra-Shield Polyester Soft

10. 	Roof Insulation (optional): Type and thickness depend on the type of building, roof deck, and local building codes and energy savings requirements.  Acceptable insulation boards include fiberglass, asphalt impregnated recovery board, foam glass or isocyanurate board.  Insulation board subject to heat or solvent attack, including polystyrene, is not acceptable.  All insulation boards must have a facer and be attached to the roof deck with FM approved fasteners.

11.	Wood Nailers:  Wood nailers used to construct flashing details must be pressure treated to improve fire and rot resistance.

12.	Roofing Granules

6.0	INSPECTION

A. 	A pre-job conference between the owner and applicator shall be conducted prior to the start of the wateproofing installation.

B.	The applicator shall inspect the substrate prior to the waterproofing application to verify that there are no conditions, which will inhibit the proper application of the waterproofing system.

7.0  	CLEANING AND SURFACE PREPARATION

A. 	The substrate must be structurally sound.  Surfaces to be waterproofed should be swept, dry, reasonably smooth and free of dust, dirt, voids, cracks, sharp projections, oil and grease  Cracks in excess of 1/16” wide should be reinforced with polyester fabric during the application of the primary waterproofing system.

B. 	The application surface should be primed with GMX Quick Drying Primer or equivalent at a rate of one gallon per 100 sq. ft.  Reinforce inside and outside corners, cracks, and construction joints with a minimum 6 inch wide piece of polyester fabric embedded in the waterproofing membrane.

C. 	Flash large cracks, expansion joints and similar details as per the recommendation outlined in the current edition of the N.R.C.A. manual.

8.0	ROOF SYSTEM INSTALLATION

A.	Optional:  Apply Ultra-Shield Primer over the roof surface at a rate of one to one and one half (1.0-1.5) gallons per 100 sq. ft.  Permit the primer to dry completely before installing the roof system.

B.	Membrane installation shall begin at the low end of the roof.  Apply GMX Hot Applied Asphalt at a rate of 60 lbs. per 100 sq. ft.

C.	Optional:  If GMX Hot Applied Polyester Plus Fabric is to be embedded in the asphalt in a ribbon 44-46 inches wide at the rate of approximately 40 lbs. per 100 sq. ft.  The roof surface must be completely covered to insure full adhesion of the polyester fabric.  Embed a full width roll of GMX Hot-Applied Polyester into the asphalt and brush firmly into place.

D.	Optional:  Glaze coat with an additional layer of GMX Hot Asphalt at a rate of fifteen (15) lbs. per 100 sq. ft. Squeegee apply the SEBS Asphalt to ensure a smooth, coated surface.  Continue across the field of the roof in a similar fashion lapping each successive full width roll of polyester fabric a minimum of six (6) inches.

E.	Install the membrane system up onto the vertical flashing surfaces restored as outlined previously in the specification.

- Allow the system to cure until it is tack free and will support foot traffic without deformation.

9.0	FINAL SURFACING

GRANULE SURFACING

- Apply a uniform layer of GMX Hot Applied Asphalt over the entire roof surfacing at a rate of 25-30 lbs. per 100 sq. ft.  The granules should be applied at a minimum rate of forty to sixty (40-60) pounds per 100 sq. ft.

NON-FIBERED ALUMINUM COATED SURFACE

- After the roof system has cured for a minimum 60 days.  Apply a top coating of Ultra-Shield Non-Fibered Aluminum Coating at a rate of one-half gallon per 100 sq. ft.

FIBERED ALUMINUM COATED SURFACE

- After the roof system has cured for a minimum 60 days.  Apply a top coating of Ultra-Shield Fibered Aluminum Coating over the entire roof surface at a rate of two gallons per 100 sq. ft.

END OF SECTION